MRE-2XCH 150/250V XLPE Insulated, LSOH (SHF1) Sheathed, Armoured Flame Retardant Instrumentation & Control Cables (Multipair/Multitriple)

Application

These armoured cables are used on board of ships in all locations for ﬁxed installations complying with IEC standards 60092-352. These cables are flame retardant, low smoke & halogen free, suitable for installations on passenger ships, as on other commercial vessels.

Standards

	IEC 60092-350/351/376/359

	IEC 60332-1

	IEC 60332-3-22

	IEC 60754-1/2

	IEC 61034

Stranded Copper Conductor XLPE Insulation

Lapping

Copper Wire Braid Armour LSOH (SHF1) Sheath

Construction

- Conductors: Class 2 stranded copper conductor.

- Insulation: XLPE.

- Cabling Element: Pair/Triple.

- Inner Covering: Lapped polyester tape.

- Armour: Copper wire braid.

- Outer Sheath: LSOH (SHF1). SHF2 can be offered upon request.

Core Identification

Pair: White/blue with printed pair number and core number. Triple: White/blue/red with printed triple number.

Mechanical and Thermal Properties

Bending Radius for Fixed Installations: 6×OD Temperature Range: -30℃ ~ +80℃

Dimensions and Weight

| Part No. | Construction No. of elements×No. of cores in element×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MRE-2XCH-1P0.75 | 1×2×0.75 | 0.5 | 1.2 | 8.1 | 90 |
| MRE-2XCH-2P0.75 | 2×2×0.75 | 0.5 | 1.3 | 9.3 | 130 |
| MRE-2XCH-3P0.75 | 3×2×0.75 | 0.5 | 1.4 | 12.4 | 200 |
| MRE-2XCH-4P0.75 | 4×2×0.75 | 0.5 | 1.4 | 13.1 | 230 |
| MRE-2XCH-5P0.75 | 5×2×0.75 | 0.5 | 1.8 | 15.2 | 320 |
| MRE-2XCH-6P0.75 | 6×2×0.75 | 0.5 | 1.8 | 16.1 | 350 |
| MRE-2XCH-7P0.75 | 7×2×0.75 | 0.5 | 1.8 | 16.1 | 370 |
| MRE-2XCH-8P0.75 | 8×2×0.75 | 0.5 | 1.9 | 17.2 | 420 |
| MRE-2XCH-10P0.75 | 10×2×0.75 | 0.5 | 1.9 | 19.1 | 500 |
| MRE-2XCH-12P0.75 | 12×2×0.75 | 0.5 | 2.0 | 20.0 | 560 |
| MRE-2XCH-14P0.75 | 14×2×0.75 | 0.5 | 2.0 | 20.6 | 610 |
| MRE-2XCH-16P0.75 | 16×2×0.75 | 0.5 | 2.1 | 22.2 | 690 |
| MRE-2XCH-19P0.75 | 19×2×0.75 | 0.5 | 2.1 | 23.6 | 790 |
| MRE-2XCH-20P0.75 | 20×2×0.75 | 0.5 | 2.1 | 23.6 | 800 |
| MRE-2XCH-24P0.75 | 24×2×0.75 | 0.5 | 2.2 | 26.8 | 980 |
| MRE-2XCH-30P0.75 | 30×2×0.75 | 0.5 | 2.3 | 29.1 | 1160 |
| MRE-2XCH-37P0.75 | 37×2×0.75 | 0.5 | 2.4 | 31.1 | 1360 |
| MRE-2XCH-1P1.0 | 1×2×1.0 | 0.5 | 1.3 | 8.7 | 110 |
| MRE-2XCH-2P1.0 | 2×2×1.0 | 0.5 | 1.3 | 9.7 | 150 |
| MRE-2XCH-3P1.0 | 3×2×1.0 | 0.5 | 1.4 | 13.2 | 230 |
| MRE-2XCH-4P1.0 | 4×2×1.0 | 0.5 | 1.8 | 14.6 | 310 |
| MRE-2XCH-5P1.0 | 5×2×1.0 | 0.5 | 1.8 | 16.1 | 360 |
| MRE-2XCH-6P1.0 | 6×2×1.0 | 0.5 | 1.9 | 17.3 | 420 |
| MRE-2XCH-7P1.0 | 7×2×1.0 | 0.5 | 1.9 | 17.3 | 440 |
| MRE-2XCH-8P1.0 | 8×2×1.0 | 0.5 | 1.9 | 18.3 | 490 |
| MRE-2XCH-10P1.0 | 10×2×1.0 | 0.5 | 2.0 | 20.5 | 590 |
| MRE-2XCH-12P1.0 | 12×2×1.0 | 0.5 | 2.0 | 21.3 | 660 |
| MRE-2XCH-14P1.0 | 14×2×1.0 | 0.5 | 2.1 | 22.2 | 730 |
| MRE-2XCH-16P1.0 | 16×2×1.0 | 0.5 | 2.1 | 23.7 | 820 |
| MRE-2XCH-19P1.0 | 19×2×1.0 | 0.5 | 2.2 | 25.4 | 940 |

| Part No. | Construction No. of elements×No. of cores in element×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MRE-2XCH-20P1.0 | 20×2×1.0 | 0.5 | 2.2 | 25.4 | 960 |
| MRE-2XCH-24P1.0 | 24×2×1.0 | 0.5 | 2.3 | 28.9 | 1170 |
| MRE-2XCH-30P1.0 | 30×2×1.0 | 0.5 | 2.4 | 31.3 | 1400 |
| MRE-2XCH-37P1.0 | 37×2×1.0 | 0.5 | 2.5 | 33.5 | 1640 |
| MRE-2XCH-1P1.5 | 1×2×1.5 | 0.6 | 1.3 | 9.7 | 140 |
| MRE-2XCH-2P1.5 | 2×2×1.5 | 0.6 | 1.3 | 10.9 | 190 |
| MRE-2XCH-3P1.5 | 3×2×1.5 | 0.6 | 1.8 | 15.7 | 340 |
| MRE-2XCH-4P1.5 | 4×2×1.5 | 0.6 | 1.9 | 16.8 | 400 |
| MRE-2XCH-5P1.5 | 5×2×1.5 | 0.6 | 1.9 | 18.6 | 480 |
| MRE-2XCH-6P1.5 | 6×2×1.5 | 0.6 | 2.0 | 20.0 | 550 |
| MRE-2XCH-7P1.5 | 7×2×1.5 | 0.6 | 2.0 | 20.0 | 590 |
| MRE-2XCH-8P1.5 | 8×2×1.5 | 0.6 | 2.0 | 21.2 | 650 |
| MRE-2XCH-10P1.5 | 10×2×1.5 | 0.6 | 2.1 | 23.8 | 800 |
| MRE-2XCH-12P1.5 | 12×2×1.5 | 0.6 | 2.2 | 24.9 | 900 |
| MRE-2XCH-14P1.5 | 14×2×1.5 | 0.6 | 2.2 | 25.8 | 990 |
| MRE-2XCH-16P1.5 | 16×2×1.5 | 0.6 | 2.3 | 27.8 | 1130 |
| MRE-2XCH-19P1.5 | 19×2×1.5 | 0.6 | 2.3 | 29.6 | 1290 |
| MRE-2XCH-20P1.5 | 20×2×1.5 | 0.6 | 2.3 | 29.6 | 1320 |
| MRE-2XCH-24P1.5 | 24×2×1.5 | 0.6 | 2.5 | 33.9 | 1630 |
| MRE-2XCH-30P1.5 | 30×2×1.5 | 0.6 | 2.8 | 37.3 | 2040 |
| MRE-2XCH-37P1.5 | 37×2×1.5 | 0.6 | 2.9 | 39.9 | 2390 |
| MRE-2XCH-1T0.75 | 1×3×0.75 | 0.5 | 1.3 | 8.7 | 110 |
| MRE-2XCH-2T0.75 | 2×3×0.75 | 0.5 | 1.4 | 12.6 | 210 |
| MRE-2XCH-3T0.75 | 3×3×0.75 | 0.5 | 1.4 | 13.3 | 240 |
| MRE-2XCH-4T0.75 | 4×3×0.75 | 0.5 | 1.8 | 15.2 | 330 |
| MRE-2XCH-5T0.75 | 5×3×0.75 | 0.5 | 1.9 | 16.8 | 400 |
| MRE-2XCH-6T0.75 | 6×3×0.75 | 0.5 | 1.9 | 18.6 | 470 |
| MRE-2XCH-7T0.75 | 7×3×0.75 | 0.5 | 1.9 | 18.6 | 490 |
| MRE-2XCH-8T0.75 | 8×3×0.75 | 0.5 | 2.0 | 20.0 | 560 |
| MRE-2XCH-10T0.75 | 10×3×0.75 | 0.5 | 2.1 | 22.5 | 690 |
| MRE-2XCH-12T0.75 | 12×3×0.75 | 0.5 | 2.1 | 23.6 | 770 |
| MRE-2XCH-14T0.75 | 14×3×0.75 | 0.5 | 2.1 | 24.5 | 850 |
| MRE-2XCH-16T0.75 | 16×3×0.75 | 0.5 | 2.2 | 26.1 | 950 |
| MRE-2XCH-19T0.75 | 19×3×0.75 | 0.5 | 2.3 | 28.2 | 1100 |
| MRE-2XCH-20T0.75 | 20×3×0.75 | 0.5 | 2.3 | 28.6 | 1140 |
| MRE-2XCH-24T0.75 | 24×3×0.75 | 0.5 | 2.4 | 31.1 | 1340 |
| MRE-2XCH-30T0.75 | 30×3×0.75 | 0.5 | 2.5 | 34.3 | 1620 |
| MRE-2XCH-32T0.75 | 32×3×0.75 | 0.5 | 2.5 | 35.4 | 1720 |
| MRE-2XCH-1T1.0 | 1×3×1.0 | 0.5 | 1.3 | 9.1 | 130 |

| Part No. | Construction No. of elements×No. of cores in element×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MRE-2XCH-2T1.0 | 2×3×1.0 | 0.5 | 1.4 | 13.4 | 240 |
| MRE-2XCH-3T1.0 | 3×3×1.0 | 0.5 | 1.8 | 14.9 | 320 |
| MRE-2XCH-4T1.0 | 4×3×1.0 | 0.5 | 1.8 | 16.1 | 380 |
| MRE-2XCH-5T1.0 | 5×3×1.0 | 0.5 | 1.9 | 17.8 | 460 |
| MRE-2XCH-6T1.0 | 6×3×1.0 | 0.5 | 2.0 | 20.0 | 560 |
| MRE-2XCH-7T1.0 | 7×3×1.0 | 0.5 | 2.0 | 20.0 | 590 |
| MRE-2XCH-8T1.0 | 8×3×1.0 | 0.5 | 2.0 | 21.3 | 660 |
| MRE-2XCH-10T1.0 | 10×3×1.0 | 0.5 | 2.1 | 24.0 | 810 |
| MRE-2XCH-12T1.0 | 12×3×1.0 | 0.5 | 2.2 | 25.4 | 920 |
| MRE-2XCH-14T1.0 | 14×3×1.0 | 0.5 | 2.2 | 26.4 | 1020 |
| MRE-2XCH-16T1.0 | 16×3×1.0 | 0.5 | 2.3 | 28.1 | 1150 |
| MRE-2XCH-19T1.0 | 19×3×1.0 | 0.5 | 2.4 | 30.3 | 1330 |
| MRE-2XCH-20T1.0 | 20×3×1.0 | 0.5 | 2.4 | 30.8 | 1380 |
| MRE-2XCH-24T1.0 | 24×3×1.0 | 0.5 | 2.5 | 33.5 | 1620 |
| MRE-2XCH-30T1.0 | 30×3×1.0 | 0.5 | 2.8 | 37.5 | 2060 |
| MRE-2XCH-32T1.0 | 32×3×1.0 | 0.5 | 2.9 | 38.9 | 2190 |
| MRE-2XCH-1T1.5 | 1×3×1.5 | 0.6 | 1.3 | 10.2 | 160 |
| MRE-2XCH-2T1.5 | 2×3×1.5 | 0.6 | 1.8 | 16.0 | 350 |
| MRE-2XCH-3T1.5 | 3×3×1.5 | 0.6 | 1.9 | 17.1 | 430 |
| MRE-2XCH-4T1.5 | 4×3×1.5 | 0.6 | 1.9 | 18.6 | 510 |
| MRE-2XCH-5T1.5 | 5×3×1.5 | 0.6 | 2.0 | 20.6 | 620 |
| MRE-2XCH-6T1.5 | 6×3×1.5 | 0.6 | 2.1 | 23.2 | 750 |
| MRE-2XCH-7T1.5 | 7×3×1.5 | 0.6 | 2.1 | 23.2 | 800 |
| MRE-2XCH-8T1.5 | 8×3×1.5 | 0.6 | 2.2 | 24.9 | 900 |
| MRE-2XCH-10T1.5 | 10×3×1.5 | 0.6 | 2.3 | 28.1 | 1110 |
| MRE-2XCH-12T1.5 | 12×3×1.5 | 0.6 | 2.3 | 29.6 | 1260 |
| MRE-2XCH-14T1.5 | 14×3×1.5 | 0.6 | 2.4 | 31.0 | 1410 |
| MRE-2XCH-16T1.5 | 16×3×1.5 | 0.6 | 2.5 | 33.0 | 1590 |
| MRE-2XCH-19T1.5 | 19×3×1.5 | 0.6 | 2.5 | 35.4 | 1830 |
| MRE-2XCH-20T1.5 | 20×3×1.5 | 0.6 | 2.8 | 36.7 | 2010 |
| MRE-2XCH-24T1.5 | 24×3×1.5 | 0.6 | 2.9 | 39.9 | 2360 |
| MRE-2XCH-30T1.5 | 30×3×1.5 | 0.6 | 3.1 | 44.2 | 2880 |
| MRE-2XCH-32T1.5 | 32×3×1.5 | 0.6 | 3.1 | 45.7 | 3060 |