BS 6883&BS 7917 Caledonian Offshore & Marine Cables

LV Flame Retardant Power & Control Cables

www.caledonian-cables.co.uk

/1kV HF-EPR Insulated, SW2/SW4 Sheathed Unarmoured Flame Retardant Power & Control Cables

Application

These elastomeric insulated cables are designed for fixed wiring in ships and on mobile offshore units, suitable for use in power and control applications.

Standards

	BS 6883

IEC 60332-3A Flame retardant

	IEC 60754-1; IEC 60754-2

Corrosivity

IEC 61034-2 Smoke density

Cold bend and impact (-40癈) (on request)

CSA C22.2 No. 38-95 (on request)

Construction

Stranded Tinned Copper Conductor HF-EPR GP4 Insulation

SW2/SW4 Outer Sheath

Conductor: Tinned copper wire stranded circular cl. 2 BS 6360/IEC 60228.

Insulation: HF-EPR GP4 according to BS 7655 1.2.

Sheath: Halogen free thermosetting compound SW4 according to BS 7655 2.6 or reduced halogen thermosetting compound SW2 according to BS 7655 2.6.

Mechanical and Thermal Properties

Minimum Internal Bending Radius: 6×OD (OD>25mm); 4×OD (OD ≤25mm) Temperature Range: -40℃ ~ +90℃

18	ADDISON	www.addison-cables.com

BS 6883&BS 7917 Caledonian Offshore & Marine Cables

LV Flame Retardant Power & Control Cables

www.caledonian-cables.co.uk

Dimensions and Weight

Single core cables

| Construction No. of cores�Cross section(mm�) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Minimum Overall Diameter mm | Maximum Overall Diameter mm | Approx. Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| 1�4 | 1.0 | 1.0 | 6.3 | 7.6 | 85 |
| 1�6 | 1.0 | 1.0 | 6.8 | 8.1 | 120 |
| 1�10 | 1.0 | 1.0 | 7.7 | 9.1 | 165 |
| 1�16 | 1.0 | 1.1 | 8.9 | 10.3 | 230 |
| 1�25 | 1.2 | 1.2 | 11.1 | 12.8 | 345 |
| 1�35 | 1.2 | 1.2 | 12.0 | 13.7 | 445 |
| 1�50 | 1.4 | 1.3 | 13.7 | 15.5 | 600 |
| 1�70 | 1.4 | 1.3 | 15.5 | 17.4 | 810 |
| 1�95 | 1.6 | 1.4 | 17.7 | 19.8 | 1100 |
| 1�120 | 1.6 | 1.5 | 19.6 | 22.0 | 1360 |
| 1�150 | 1.8 | 1.6 | 21.6 | 24.2 | 1650 |
| 1�185 | 2.0 | 1.7 | 24.0 | 26.6 | 2070 |
| 1�240 | 2.2 | 1.8 | 27.1 | 29.9 | 2670 |
| 1�300 | 2.4 | 1.9 | 30.0 | 33.2 | 3340 |

Multicore cables

| Construction No. of cores�Cross section(mm�) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Minimum Overall Diameter mm | Maximum Overall Diameter mm | Approx. Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| 2�1 | 0.8 | 1.0 | 7.5 | 8.8 | 100 |
| 2�1.5 | 0.8 | 1.1 | 8.2 | 9.6 | 125 |
| 2�2.5 | 0.8 | 1.1 | 9.0 | 10.4 | 160 |
| 2�4 | 1.0 | 1.2 | 11.0 | 12.7 | 235 |
| 2�6 | 1.0 | 1.2 | 12.1 | 13.8 | 300 |
| 2�10 | 1.0 | 1.3 | 14.1 | 15.9 | 415 |
| 2�16 | 1.0 | 1.4 | 16.3 | 18.3 | 590 |
| 2�25 | 1.2 | 1.5 | 20.4 | 22.9 | 890 |
| 2�35 | 1.2 | 1.6 | 22.4 | 24.9 | 1150 |
| 2�50 | 1.4 | 1.7 | 25.7 | 28.4 | 1570 |
| 2�70 | 1.4 | 1.9 | 29.6 | 32.7 | 2140 |
| 2�95 | 1.6 | 2.1 | 34.1 | 37.4 | 2930 |
| 2�120 | 1.6 | 2.2 | 37.7 | 41.1 | 3600 |
| 3�1 | 0.8 | 1.1 | 8.2 | 9.5 | 110 |
| 3�1.5 | 0.8 | 1.1 | 8.7 | 10.1 | 150 |
| 3�2.5 | 0.8 | 1.1 | 9.6 | 11.0 | 190 |
| 3�4 | 1.0 | 1.2 | 11.7 | 13.4 | 280 |
| 3�6 | 1.0 | 1.2 | 12.9 | 14.7 | 370 |
| 3�10 | 1.0 | 1.3 | 15.0 | 17.0 | 505 |
| 3�16 | 1.0 | 1.4 | 17.4 | 19.4 | 750 |

www.addison-cables.com

ADDISON	19

BS 6883&BS 7917 Caledonian Offshore & Marine Cables

LV Flame Retardant Power & Control Cables

www.caledonian-cables.co.uk

| Construction No. of cores�Cross section(mm�) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Minimum Overall Diameter mm | Maximum Overall Diameter mm | Approx. Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| 3�25 | 1.2 | 1.6 | 22.0 | 24.6 | 1150 |
| 3�35 | 1.2 | 1.7 | 24.1 | 26.7 | 1490 |
| 3�50 | 1.4 | 1.8 | 27.7 | 30.5 | 2030 |
| 3�70 | 1.4 | 2.0 | 31.8 | 35.1 | 2790 |
| 3�95 | 1.6 | 2.2 | 36.7 | 40.1 | 3820 |
| 3�120 | 1.6 | 2.3 | 40.5 | 44.4 | 4710 |
| 3�150 | 1.8 | 2.5 | 44.9 | 49.0 | 5710 |
| 3�185 | 2.0 | 2.7 | 50.1 | 54.6 | 7180 |
| 3�240 | 2.2 | 2.9 | 56.7 | 61.5 | 9310 |
| 3�300 | 2.4 | 3.2 | 63.1 | 68.6 | 10860 |
| 4�1 | 0.8 | 1.1 | 8.9 | 10.3 | 140 |
| 4�1.5 | 0.8 | 1.1 | 9.5 | 10.9 | 175 |
| 4�2.5 | 0.8 | 1.1 | 10.5 | 12.1 | 225 |
| 4�4 | 1.0 | 1.2 | 12.9 | 14.6 | 340 |
| 4�6 | 1.0 | 1.3 | 14.4 | 16.2 | 465 |
| 4�10 | 1.0 | 1.4 | 16.7 | 18.7 | 640 |
| 4�16 | 1.0 | 1.5 | 19.4 | 21.8 | 960 |
| 4�25 | 1.2 | 1.7 | 24.5 | 27.1 | 1550 |
| 4�35 | 1.2 | 1.8 | 26.8 | 29.5 | 1920 |
| 4�50 | 1.4 | 1.9 | 30.8 | 34.0 | 2600 |
| 4�70 | 1.4 | 2.1 | 35.4 | 38.8 | 3570 |
| 4�95 | 1.6 | 2.3 | 40.8 | 44.7 | 4900 |
| 4�120 | 1.6 | 2.5 | 45.2 | 49.3 | 6070 |
| 4�150 | 1.8 | 2.7 | 50.1 | 54.7 | 7360 |
| 4�185 | 2.0 | 2.9 | 55.8 | 60.7 | 9260 |
| 4�240 | 2.2 | 3.2 | 63.4 | 68.9 | 12030 |
| 5�1.5 | 0.8 | 1.1 | 10.4 | 12.0 | 200 |
| 7�1.5 | 0.8 | 1.2 | 11.5 | 13.2 | 255 |
| 12�1.5 | 0.8 | 1.3 | 15.2 | 17.2 | 405 |
| 19�1.5 | 0.8 | 1.4 | 18.0 | 20.1 | 600 |
| 27�1.5 | 0.8 | 1.6 | 21.9 | 24.5 | 850 |
| 37�1.5 | 0.8 | 1.7 | 24.7 | 27.3 | 1120 |
| 5�2.5 | 0.8 | 1.2 | 11.7 | 13.3 | 270 |
| 7�2.5 | 0.8 | 1.2 | 12.7 | 14.4 | 335 |
| 12�2.5 | 0.8 | 1.4 | 17.1 | 19.1 | 550 |
| 19�2.5 | 0.8 | 1.5 | 20.2 | 22.7 | 830 |

20	ADDISON	www.addison-cables.com