Water Blocked S3 or S3/S7 BFOU(i) 250V

Applications

These cables are partially water blocked, fire resistant, flame retardant, low smoke, halogen free and mud resistant, used for instrumentation, communication, control and alarm systems.

Standards

	IEC 60092-376

	IEC 60092-351

	IEC 60092-359

	IEC 60331-21

	IEC 60332-1

	IEC 60332-3-22

	IEC 60754-1,2

	IEC 61034-1,2

	NEK 606:2004

- VG 95218 part 29

Construction

SHF2 Inner Sheath Copper Wire Braid

Copper/Polyester Tape + Drain Wire Water Blocking Fillers

Mica Tape + HFEPR Insulation Stranded Copper Conductor Halogen-free Bedding

Water Blocking tape

Polyurethane Outer Sheath

- Conductors: Circular tinned annealed stranded copper wire to IEC 60228 class 2.

- Insulation: Mica tape + Halogen free EPR compound.

- Twinning: Colour coded cores twisted together.

- Filler: Water blocking fillers, if required.

- Individual Shielding: Each pairs/triples are screened by copper backed polyester tape in contact with a stranded tinned copper drain wire and wrapped with polyester tape. Pairs/triples are numbered with numbered tape or by numbers printed directly on the insulated conductors.

- Filler: Water blocking fillers, if required.

- Bedding: Halogen free compound, PETP wrapping tape will be applied over the bedding, if required.

- Armour: Tinned copper wire braid, PETP wrapping tape will be applied over the

braiding, if required.

- Water Blocking Elements: Water blocking tape and strings for providing longitudinal

water tightness.

  - Inner Sheath: Halogen free thermosetting compound, SHF2 (for TYPE S3). Halogen free MUD resistant thermosetting compound, SHF MUD (for TYPE S3/S7), coloured grey (blue for intrinsically safe).

  - Outer Sheath: Polyurethane for providing transversal water tightness, PE is optional,but can not meet low smoke standard.

Electrical Characteristics

| Nominal Cross Section Area | mm² | 0.75 | 1.0 | 1.5 | 2.5 |
| --- | --- | --- | --- | --- | --- |
| Nominal Conductor Diameter | mm | 1.1 | 1.3 | 1.6 | 2.0 |
| Maximum Resistant@20˚C | Ω/km | 26.3 | 19.3 | 12.9 | 8.02 |
| Mutual Capacitance | nF/km | 85 | 95 | 100 | 110 |
| Nominal Inductance@1KHz | MH/km | 0.731 | 0.691 | 0.673 | 0.629 |
| Maximum L/R@1KHz | μH/Ω | 20 | 25 | 35 | 55 |
| Operating Voltage | V | 250 | 250 | 250 | 250 |

Mechanical and Thermal Properties

  - Bending Radius: 8×OD (during installation); 6×OD (fixed installed)

  - Temperature Range: -20˚C ~ +90˚C

Dimensions and Weight

| Construction No. of elements×No. of cores in element×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Inner Sheath Thickness mm | Nominal Outer Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- | --- |
| 1×2×0.75 | 0.6 | 1.1 | 1.2 | 1.0 | 14.1±2 | 236 |
| 2×2×0.75 | 0.6 | 1.1 | 1.3 | 1.0 | 18.7±2 | 425 |
| 3×2×0.75 | 0.6 | 1.1 | 1.4 | 1.0 | 19.5±2 | 567 |
| 4×2×0.75 | 0.6 | 1.1 | 1.4 | 1.0 | 20.6±2 | 641 |
| 5×2×0.75 | 0.6 | 1.1 | 1.5 | 1.0 | 22.2±2 | 740 |
| 6×2×0.75 | 0.6 | 1.1 | 1.5 | 1.0 | 23.7±2 | 845 |
| 7×2×0.75 | 0.6 | 1.1 | 1.5 | 1.0 | 23.7±2 | 872 |
| 8×2×0.75 | 0.6 | 1.1 | 1.6 | 1.0 | 25.6±2 | 950 |
| 9×2×0.75 | 0.6 | 1.1 | 1.7 | 1.0 | 27.1±2 | 1050 |
| 10×2×0.75 | 0.6 | 1.1 | 1.7 | 1.0 | 28.2±2 | 1082 |
| 12×2×0.75 | 0.6 | 1.1 | 1.7 | 1.0 | 28.8±2 | 1202 |
| 14×2×0.75 | 0.6 | 1.1 | 1.8 | 1.0 | 30.2±2 | 1265 |

| Construction No. of elements×No. of cores in element×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Inner Sheath Thickness mm | Nominal Outer Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- | --- |
| 15×2×0.75 | 0.6 | 1.1 | 1.8 | 1.0 | 32.0±2 | 1370 |
| 16×2×0.75 | 0.6 | 1.1 | 1.9 | 1.0 | 32.6±2 | 1486 |
| 18×2×0.75 | 0.6 | 1.1 | 1.9 | 1.0 | 34.1±2 | 1549 |
| 19×2×0.75 | 0.6 | 1.2 | 1.9 | 1.0 | 34.7±2 | 1654 |
| 20×2×0.75 | 0.6 | 1.2 | 2.0 | 1.0 | 36.1±2 | 1785 |
| 21×2×0.75 | 0.6 | 1.2 | 2.0 | 1.0 | 37.0±2 | 1853 |
| 23×2×0.75 | 0.6 | 1.2 | 2.0 | 1.0 | 37.5±2 | 1990 |
| 24×2×0.75 | 0.6 | 1.2 | 2.1 | 1.0 | 39.7±2 | 2079 |
| 27×2×0.75 | 0.6 | 1.2 | 2.2 | 1.0 | 40.7±2 | 2273 |
| 30×2×0.75 | 0.6 | 1.2 | 2.2 | 1.0 | 41.9±2 | 2452 |
| 33×2×0.75 | 0.6 | 1.2 | 2.3 | 1.0 | 43.5±2 | 2662 |
| 37×2×0.75 | 0.6 | 1.2 | 2.3 | 1.0 | 44.7±2 | 2861 |
| 1×3×0.75 | 0.6 | 1.1 | 1.1 | 1.0 | 13.9±2 | 257 |
| 2×3×0.75 | 0.6 | 1.1 | 1.4 | 1.0 | 17.5±2 | 441 |
| 3×3×0.75 | 0.6 | 1.1 | 1.4 | 1.0 | 20.4±2 | 609 |
| 4×3×0.75 | 0.6 | 1.1 | 1.4 | 1.0 | 21.7±2 | 709 |
| 7×3×0.75 | 0.6 | 1.1 | 1.6 | 1.0 | 25.6±2 | 1008 |
| 8×3×0.75 | 0.6 | 1.1 | 1.7 | 1.0 | 27.0±2 | 1029 |
| 12×3×0.75 | 0.6 | 1.3 | 1.8 | 1.0 | 31.6±2 | 1507 |
| 16×3×0.75 | 0.6 | 1.4 | 1.9 | 1.0 | 34.6±2 | 1859 |
| 19×3×0.75 | 0.6 | 1.4 | 2.1 | 1.0 | 36.4±2 | 2084 |
| 24×3×0.75 | 0.6 | 1.8 | 2.2 | 1.0 | 41.6±2 | 2709 |
| 1×2×1.0 | 0.6 | 1.1 | 1.2 | 1.0 | 14.5±2 | 257 |
| 2×2×1.0 | 0.6 | 1.1 | 1.4 | 1.0 | 19.6±2 | 473 |
| 3×2×1.0 | 0.6 | 1.1 | 1.4 | 1.0 | 20.3±2 | 630 |
| 4×2×1.0 | 0.6 | 1.1 | 1.4 | 1.0 | 21.3±2 | 656 |
| 5×2×1.0 | 0.6 | 1.1 | 1.5 | 1.0 | 23.1±2 | 966 |
| 6×2×1.0 | 0.6 | 1.1 | 1.6 | 1.0 | 24.8±2 | 998 |
| 7×2×1.0 | 0.6 | 1.1 | 1.6 | 1.0 | 24.8±2 | 903 |
| 8×2×1.0 | 0.6 | 1.1 | 1.6 | 1.0 | 26.7±2 | 1034 |
| 9×2×1.0 | 0.6 | 1.1 | 1.7 | 1.0 | 28.3±2 | 1192 |
| 10×2×1.0 | 0.6 | 1.1 | 1.7 | 1.0 | 29.4±2 | 1229 |
| 12×2×1.0 | 0.6 | 1.1 | 1.8 | 1.0 | 30.3±2 | 1365 |
| 14×2×1.0 | 0.6 | 1.1 | 1.8 | 1.0 | 31.5±2 | 1449 |
| 15×2×1.0 | 0.6 | 1.1 | 1.9 | 1.0 | 33.6±2 | 1586 |
| 16×2×1.0 | 0.6 | 1.1 | 1.9 | 1.0 | 34.1±2 | 1701 |
| 18×2×1.0 | 0.6 | 1.2 | 2.0 | 1.0 | 36.2±2 | 1832 |
| 19×2×1.0 | 0.6 | 1.2 | 2.0 | 1.0 | 36.5±2 | 1922 |
| 20×2×1.0 | 0.6 | 1.2 | 2.1 | 1.0 | 38.0±2 | 2074 |
| 21×2×1.0 | 0.6 | 1.2 | 2.1 | 1.0 | 39.3±2 | 2242 |

| Construction No. of elements×No. of cores in element×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Inner Sheath Thickness mm | Nominal Outer Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- | --- |
| 23×2×1.0 | 0.6 | 1.2 | 2.1 | 1.0 | 39.9±2 | 2410 |
| 24×2×1.0 | 0.6 | 1.2 | 2.2 | 1.0 | 41.8±2 | 2452 |
| 27×2×1.0 | 0.6 | 1.2 | 2.2 | 1.0 | 42.6±2 | 2625 |
| 30×2×1.0 | 0.6 | 1.2 | 2.3 | 1.0 | 44.1±2 | 2856 |
| 33×2×1.0 | 0.6 | 1.2 | 2.3 | 1.0 | 45.6±2 | 3087 |
| 37×2×1.0 | 0.6 | 1.4 | 2.4 | 1.0 | 47.4±2 | 3392 |
| 1×3×1.0 | 0.6 | 1.1 | 1.2 | 1.0 | 14.6±2 | 289 |
| 2×3×1.0 | 0.6 | 1.1 | 1.4 | 1.0 | 20.8±2 | 672 |
| 3×3×1.0 | 0.6 | 1.1 | 1.5 | 1.0 | 21.3±2 | 698 |
| 4×3×1.0 | 0.6 | 1.1 | 1.5 | 1.0 | 22.9±2 | 814 |
| 5×3×1.0 | 0.6 | 1.1 | 1.6 | 1.0 | 24.8±2 | 1013 |
| 6×3×1.0 | 0.6 | 1.1 | 1.7 | 1.0 | 27.4±2 | 1192 |
| 7×3×1.0 | 0.6 | 1.1 | 1.7 | 1.0 | 27.4±2 | 1239 |
| 8×3×1.0 | 0.6 | 1.1 | 1.7 | 1.0 | 29.0±2 | 1334 |
| 9×3×1.0 | 0.6 | 1.1 | 1.8 | 1.0 | 30.9±2 | 1523 |
| 10×3×1.0 | 0.6 | 1.1 | 1.9 | 1.0 | 33.1±2 | 1528 |
| 12×3×1.0 | 0.6 | 1.1 | 1.9 | 1.0 | 34.0±2 | 1769 |
| 14×3×1.0 | 0.6 | 1.2 | 2.0 | 1.0 | 35.8±2 | 1911 |
| 15×3×1.0 | 0.6 | 1.2 | 2.0 | 1.0 | 36.8±2 | 2032 |
| 16×3×1.0 | 0.6 | 1.2 | 2.1 | 1.0 | 38.0±2 | 2210 |
| 18×3×1.0 | 0.6 | 1.2 | 2.1 | 1.0 | 40.1±2 | 2426 |
| 19×3×1.0 | 0.6 | 1.2 | 2.2 | 1.0 | 40.6±2 | 2473 |
| 20×3×1.0 | 0.6 | 1.2 | 2.2 | 1.0 | 41.6±2 | 2720 |
| 21×3×1.0 | 0.6 | 1.2 | 2.2 | 1.0 | 42.4±2 | 2819 |
| 23×3×1.0 | 0.6 | 1.2 | 2.3 | 1.0 | 44.0±2 | 3082 |
| 24×3×1.0 | 0.6 | 1.2 | 2.3 | 1.0 | 44.8±2 | 3302 |
| 27×3×1.0 | 0.6 | 1.4 | 2.4 | 1.0 | 47.3±2 | 3418 |
| 30×3×1.0 | 0.6 | 1.4 | 2.5 | 1.0 | 49.4±2 | 3743 |
| 32×3×1.0 | 0.6 | 1.4 | 2.5 | 1.0 | 50.6±2 | 3943 |
| 1×2×1.5 | 0.7 | 1.1 | 1.2 | 1.0 | 15.5±2 | 310 |
| 2×2×1.5 | 0.7 | 1.1 | 1.4 | 1.0 | 21.2±2 | 572 |
| 3×2×1.5 | 0.7 | 1.1 | 1.5 | 1.0 | 22.2±2 | 761 |
| 4×2×1.5 | 0.7 | 1.1 | 1.5 | 1.0 | 23.5±2 | 809 |
| 5×2×1.5 | 0.7 | 1.1 | 1.6 | 1.0 | 25.4±2 | 1024 |
| 6×2×1.5 | 0.7 | 1.1 | 1.7 | 1.0 | 27.4±2 | 1187 |
| 7×2×1.5 | 0.7 | 1.1 | 1.7 | 1.0 | 27.4±2 | 1229 |
| 8×2×1.5 | 0.7 | 1.1 | 1.7 | 1.0 | 29.5±2 | 1286 |
| 9×2×1.5 | 0.7 | 1.1 | 1.8 | 1.0 | 31.4±2 | 1475 |
| 10×2×1.5 | 0.7 | 1.1 | 1.9 | 1.0 | 32.9±2 | 1512 |
| 12×2×1.5 | 0.7 | 1.1 | 1.9 | 1.0 | 33.6±2 | 1764 |

| Construction No. of elements×No. of cores in element×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Inner Sheath Thickness mm | Nominal Outer Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- | --- |
| 14×2×1.5 | 0.7 | 1.2 | 2.0 | 1.0 | 35.6±2 | 1838 |
| 15×2×1.5 | 0.7 | 1.2 | 2.1 | 1.0 | 38.0±2 | 2006 |
| 16×2×1.5 | 0.7 | 1.2 | 2.1 | 1.0 | 38.9±2 | 2158 |
| 18×2×1.5 | 0.7 | 1.2 | 2.2 | 1.0 | 40.9±2 | 2373 |
| 19×2×1.5 | 0.7 | 1.2 | 2.2 | 1.0 | 41.3±2 | 2515 |
| 20×2×1.5 | 0.7 | 1.2 | 2.2 | 1.0 | 42.8±2 | 2667 |
| 21×2×1.5 | 0.7 | 1.2 | 2.3 | 1.0 | 44.1±2 | 2793 |
| 23×2×1.5 | 0.7 | 1.2 | 2.3 | 1.0 | 44.7±2 | 3008 |
| 24×2×1.5 | 0.7 | 1.4 | 2.4 | 1.0 | 47.2±2 | 3234 |
| 27×2×1.5 | 0.7 | 1.4 | 2.4 | 1.0 | 48.1±2 | 3313 |
| 30×2×1.5 | 0.7 | 1.4 | 2.5 | 1.0 | 49.8±2 | 3612 |
| 32×2×1.5 | 0.7 | 1.4 | 2.6 | 1.0 | 51.0±2 | 3869 |
| 33×2×1.5 | 0.7 | 1.4 | 2.6 | 1.0 | 51.7±2 | 3927 |
| 37×2×1.5 | 0.7 | 1.4 | 2.6 | 1.0 | 53.2±2 | 4242 |
| 1×3×1.5 | 0.7 | 1.1 | 1.3 | 1.0 | 15.6±2 | 341 |
| 2×3×1.5 | 0.7 | 1.1 | 1.5 | 1.0 | 20.5±2 | 588 |
| 3×3×1.5 | 0.7 | 1.1 | 1.5 | 1.0 | 23.4±2 | 840 |
| 4×3×1.5 | 0.7 | 1.1 | 1.6 | 1.0 | 25.7±2 | 1024 |
| 5×3×1.5 | 0.7 | 1.1 | 1.7 | 1.0 | 27.4±2 | 1255 |
| 6×3×1.5 | 0.7 | 1.1 | 1.8 | 1.0 | 30.3±2 | 1475 |
| 7×3×1.5 | 0.7 | 1.1 | 1.8 | 1.0 | 30.3±2 | 1544 |
| 8×3×1.5 | 0.7 | 1.1 | 1.8 | 1.0 | 32.2±2 | 1664 |
| 9×3×1.5 | 0.7 | 1.2 | 1.9 | 1.0 | 34.6±2 | 1927 |
| 10×3×1.5 | 0.7 | 1.2 | 2.0 | 1.0 | 37.1±2 | 2032 |
| 12×3×1.5 | 0.7 | 1.2 | 2.1 | 1.0 | 38.8±2 | 2221 |
| 14×3×1.5 | 0.7 | 1.2 | 2.1 | 1.0 | 40.3±2 | 2478 |
| 15×3×1.5 | 0.7 | 1.2 | 2.2 | 1.0 | 41.7±2 | 2657 |
| 16×3×1.5 | 0.7 | 1.2 | 2.2 | 1.0 | 42.8±2 | 2914 |
| 18×3×1.5 | 0.7 | 1.2 | 2.3 | 1.0 | 44.9±2 | 3050 |
| 19×3×1.5 | 0.7 | 1.2 | 2.3 | 1.0 | 45.3±2 | 3360 |
| 20×3×1.5 | 0.7 | 1.4 | 2.4 | 1.0 | 46.9±2 | 3470 |
| 21×3×1.5 | 0.7 | 1.4 | 2.4 | 1.0 | 47.8±2 | 3602 |
| 23×3×1.5 | 0.7 | 1.4 | 2.5 | 1.0 | 49.7±2 | 3943 |
| 24×3×1.5 | 0.7 | 1.4 | 2.5 | 1.0 | 50.6±2 | 4121 |
| 27×3×1.5 | 0.7 | 1.4 | 2.6 | 1.0 | 53.1±2 | 4321 |
| 30×3×1.5 | 0.7 | 1.4 | 2.7 | 1.0 | 55.5±2 | 4736 |
| 32×3×1.5 | 0.7 | 1.6 | 2.8 | 1.0 | 57.5±2 | 5093 |
| 1×2×2.5 | 0.7 | 1.1 | 1.3 | 1.0 | 16.0±2 | 357 |
| 2×2×2.5 | 0.7 | 1.1 | 1.5 | 1.0 | 20.5±2 | 588 |
| 3×2×2.5 | 0.7 | 1.1 | 1.5 | 1.0 | 23.6±2 | 908 |

| Construction No. of elements×No. of cores in element×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Inner Sheath Thickness mm | Nominal Outer Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- | --- |
| 4×2×2.5 | 0.7 | 1.1 | 1.6 | 1.0 | 25.2±2 | 1061 |
| 5×2×2.5 | 0.7 | 1.1 | 1.7 | 1.0 | 27.3±2 | 1244 |
| 6×2×2.5 | 0.7 | 1.1 | 1.7 | 1.0 | 29.4±2 | 1439 |
| 7×2×2.5 | 0.7 | 1.1 | 1.7 | 1.0 | 29.4±2 | 1502 |
| 8×2×2.5 | 0.7 | 1.1 | 1.8 | 1.0 | 31.9±2 | 1638 |
| 9×2×2.5 | 0.7 | 1.1 | 1.9 | 1.0 | 33.9±2 | 1869 |
| 10×2×2.5 | 0.7 | 1.2 | 2.0 | 1.0 | 35.8±2 | 1864 |
| 12×2×2.5 | 0.7 | 1.2 | 2.0 | 1.0 | 36.6±2 | 2063 |
| 14×2×2.5 | 0.7 | 1.2 | 2.1 | 1.0 | 38.9±2 | 2389 |
| 15×2×2.5 | 0.7 | 1.2 | 2.2 | 1.0 | 41.5±2 | 2604 |
| 16×2×2.5 | 0.7 | 1.2 | 2.2 | 1.0 | 42.1±2 | 2720 |
| 18×2×2.5 | 0.7 | 1.2 | 2.3 | 1.0 | 44.3±2 | 2966 |
| 19×2×2.5 | 0.7 | 1.2 | 2.3 | 1.0 | 44.7±2 | 3077 |
| 20×2×2.5 | 0.7 | 1.4 | 2.4 | 1.0 | 46.8±2 | 3402 |
| 21×2×2.5 | 0.7 | 1.4 | 2.4 | 1.0 | 48.1±2 | 3544 |
| 23×2×2.5 | 0.7 | 1.4 | 2.5 | 1.0 | 48.9±2 | 3738 |
| 24×2×2.5 | 0.7 | 1.4 | 2.5 | 1.0 | 51.1±2 | 3843 |
| 27×2×2.5 | 0.7 | 1.4 | 2.6 | 1.0 | 52.3±2 | 4200 |
| 30×2×2.5 | 0.7 | 1.4 | 2.7 | 1.0 | 54.2±2 | 4589 |
| 33×2×2.5 | 0.7 | 1.4 | 2.7 | 1.0 | 56.1±2 | 4972 |
| 37×2×2.5 | 0.7 | 1.6 | 2.8 | 1.0 | 58.4±2 | 5486 |
| 1×3×2.5 | 0.7 | 1.1 | 1.2 | 1.0 | 16.5±2 | 399 |
| 2×3×2.5 | 0.7 | 1.1 | 1.6 | 1.0 | 24.5±2 | 998 |
| 3×3×2.5 | 0.7 | 1.1 | 1.6 | 1.0 | 25.4±2 | 1108 |
| 4×3×2.5 | 0.7 | 1.1 | 1.7 | 1.0 | 27.3±2 | 1313 |
| 5×3×2.5 | 0.7 | 1.1 | 1.7 | 1.0 | 29.4±2 | 1533 |
| 6×3×2.5 | 0.7 | 1.1 | 1.9 | 1.0 | 32.7±2 | 1822 |
| 7×3×2.5 | 0.7 | 1.1 | 1.9 | 1.0 | 32.7±2 | 1922 |
| 8×3×2.5 | 0.7 | 1.2 | 2.0 | 1.0 | 35.3±2 | 2126 |
| 9×3×2.5 | 0.7 | 1.2 | 2.0 | 1.0 | 37.4±2 | 2405 |
| 10×3×2.5 | 0.7 | 1.2 | 2.2 | 1.0 | 40.8±2 | 2525 |
| 12×3×2.5 | 0.7 | 1.2 | 2.2 | 1.0 | 42.0±2 | 2819 |
| 14×3×2.5 | 0.7 | 1.2 | 2.3 | 1.0 | 43.9±2 | 3150 |
| 15×3×2.5 | 0.7 | 1.2 | 2.3 | 1.0 | 45.1±2 | 3350 |
| 16×3×2.5 | 0.7 | 1.4 | 2.4 | 1.0 | 46.9±2 | 3591 |
| 18×3×2.5 | 0.7 | 1.4 | 2.5 | 1.0 | 49.2±2 | 3927 |
| 19×3×2.5 | 0.7 | 1.4 | 2.5 | 1.0 | 49.6±2 | 4079 |
| 20×3×2.5 | 0.7 | 1.4 | 2.5 | 1.0 | 50.9±2 | 4394 |
| 21×3×2.5 | 0.7 | 1.4 | 2.6 | 1.0 | 52.0±2 | 4589 |
| 23×3×2.5 | 0.7 | 1.4 | 2.7 | 1.0 | 54.1±2 | 4998 |

| Construction No. of elements×No. of cores in element×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Inner Sheath Thickness mm | Nominal Outer Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- | --- |
| 24×3×2.5 | 0.7 | 1.4 | 2.7 | 1.0 | 55.0±2 | 5024 |
| 27×3×2.5 | 0.7 | 1.6 | 2.8 | 1.0 | 58.2±2 | 5602 |
| 30×3×2.5 | 0.7 | 1.6 | 2.9 | 1.0 | 60.8±2 | 6148 |
| 32×3×2.5 | 0.7 | 1.6 | 3.0 | 1.0 | 62.6±2 | 6526 |

NEK 606:2004

N

Standard

Zero

Halogen Free IEC60754-1

IEC 60092-351

N

Standard

Low Corrosivity IEC60754-2

IEC 60092-376

N

Standard

Low Smoke Emission IEC 61034-1&2

IEC 60092-359

N

Standard

Flame Retardancy IEC60332-1

Water Tightness VG 95218-29

Reduced Fire Propagation IEC60332-3-22

W	E

Circuit Integrity IEC 60331-21