BS 6883&BS 7917 Caledonian Offshore & Marine Cables

MV Fire Resistant Power & Control Cables

www.caledonian-cables.co.uk

  - /3.3kV, 3.3/3.3kV HF-EPR Insulated, SW2/SW4 Sheathed Armoured Fire Resistant Power & Control Cables

Application

These fire resistant medium voltage elastomeric insulated cables are designed for fixed wiring in ships and on mobile offshore units, suitable for use in power and control applications where ﬁre integrity is essential.

Standards

	BS 7917

    - IEC 60331-31 Fire

resistant

    - IEC 60332-3A Flame

retardant

    - IEC 60754-1; IEC 60754-2 Corrosivity

    - IEC 61034-2 Smoke density

    - Cold bend and impact (-40°C) (on request)

    - CSA C22.2 No. 38-95 (on request)

Construction

Stranded Tinned Copper Conductor Mica Tape+HF-EPR GP5 Insulation SB1 Inner Sheath

Galvanized Steel Wire/Tinned Bronze Wire Braid SW2/SW4 Outer Sheath

    - Conductor: Tinned copper wire stranded circular cl. 2 BS 6360/IEC 60228.

    - Insulation: Mica tape + HF-EPR GP5 according to BS 7655 1.2.

    - Inner Sheath: Halogen free thermosetting compound SB1 according to BS 7917.

    - Armour: Galvanized steel wire braid or tinned bronze wire braid (single core).

    - Outer Sheath: Halogen free thermosetting compound SW4 according to BS 7655 2.6 or reduced halogen thermosetting compound SW2 according to BS 7655 2.6.

Mechanical and Thermal Properties

Minimum Internal Bending Radius: 6×OD Temperature Range: -40℃ ~ +90℃

www.addison-cables.com

ADDISON	15

BS 6883&BS 7917 Caledonian Offshore & Marine Cables

MV Fire Resistant Power & Control Cables

www.caledonian-cables.co.uk

Dimensions and Weight

1.9/3.3kV

| Construction No. of cores×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Inner Sheath Thickness mm | Minimum Diameter Over Inner Sheath mm | Maximum Diameter Over Inner Sheath mm | Nominal Armour Wire Diameter mm | Nominal Outer Sheath Thickness mm | Minimum Overall Diameter mm | Maximum Overall Diameter mm | Approx. Weight kg/km |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1×25 | 2.2 | 1.2 | 13.4 | 15.2 | 0.3 | 1.4 | 17.5 | 19.9 | 687 |
| 1×35 | 2.2 | 1.3 | 14.4 | 16.4 | 0.3 | 1.4 | 18.6 | 21.0 | 806 |
| 1×50 | 2.2 | 1.3 | 15.6 | 17.6 | 0.3 | 1.5 | 20.0 | 22.8 | 983 |
| 1×70 | 2.2 | 1.4 | 17.6 | 19.6 | 0.3 | 1.6 | 22.1 | 25.0 | 1283 |
| 1×95 | 2.4 | 1.5 | 19.8 | 22.3 | 0.3 | 1.7 | 24.5 | 27.6 | 1637 |
| 1×120 | 2.4 | 1.6 | 21.7 | 24.2 | 0.3 | 1.7 | 26.4 | 29.5 | 1997 |
| 1×150 | 2.4 | 1.6 | 23.2 | 25.8 | 0.45 | 1.8 | 28.8 | 32.0 | 2439 |
| 1×185 | 2.4 | 1.7 | 25.2 | 27.8 | 0.45 | 1.9 | 31.0 | 34.7 | 2933 |
| 1×240 | 2.4 | 1.8 | 27.9 | 30.7 | 0.45 | 2.0 | 33.9 | 37.7 | 3671 |
| 1×300 | 2.4 | 1.9 | 30.4 | 33.6 | 0.45 | 2.1 | 36.6 | 40.5 | 4446 |
| 1×400 | 2.6 | 2.0 | 34.1 | 37.5 | 0.45 | 2.3 | 40.7 | 45.2 | 5435 |
| 1×500 | 2.8 | 2.2 | 38.0 | 41.5 | 0.45 | 2.5 | 44.9 | 49.6 | 6746 |
| 1×630 | 2.8 | 2.3 | 41.6 | 45.6 | 0.45 | 2.6 | 48.8 | 54.0 | 8583 |
| 3×25 | 2.2 | 1.8 | 27.4 | 30.1 | 0.45 | 2.0 | 33.4 | 37.2 | 2072 |
| 3×35 | 2.2 | 1.8 | 29.3 | 32.4 | 0.45 | 2.1 | 35.5 | 39.3 | 2422 |
| 3×50 | 2.2 | 1.9 | 32.1 | 35.3 | 0.45 | 2.2 | 38.4 | 42.8 | 2977 |
| 3×70 | 2.2 | 2.1 | 36.2 | 39.6 | 0.45 | 2.4 | 42.9 | 47.5 | 3920 |
| 3×95 | 2.4 | 2.3 | 41.0 | 44.9 | 0.45 | 2.6 | 48.2 | 53.4 | 5041 |
| 3×120 | 2.4 | 2.4 | 44.9 | 48.9 | 0.45 | 2.7 | 52.2 | 57.6 | 6165 |
| 3×150 | 2.4 | 2.6 | 48.4 | 53.0 | 0.45 | 2.9 | 56.2 | 61.7 | 7333 |
| 3×185 | 2.4 | 2.7 | 52.5 | 57.2 | 0.45 | 3.0 | 60.5 | 66.6 | 8800 |
| 3×240 | 2.4 | 3.0 | 58.5 | 63.8 | 0.45 | 3.3 | 67.0 | 73.4 | 11172 |
| 3×300 | 2.4 | 3.2 | 64.0 | 69.4 | 0.45 | 3.5 | 72.8 | 79.9 | 13587 |

3.3/3.3kV

| Construction No. of cores×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Inner Sheath Thickness mm | Minimum Diameter Over Inner Sheath mm | Maximum Diameter Over Inner Sheath mm | Nominal Armour Wire Diameter mm | Nominal Outer Sheath Thickness mm | Minimum Overall Diameter mm | Maximum Overall Diameter mm | Approx. Weight kg/km |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1×25 | 3.0 | 1.3 | 15.1 | 17.1 | 0.3 | 1.5 | 19.4 | 22.3 | 789 |
| 1×35 | 3.0 | 1.3 | 16.0 | 18.0 | 0.3 | 1.5 | 20.3 | 23.2 | 900 |
| 1×50 | 3.0 | 1.4 | 17.4 | 19.4 | 0.3 | 1.6 | 21.9 | 24.8 | 1097 |
| 1×70 | 3.0 | 1.5 | 19.3 | 21.7 | 0.3 | 1.6 | 23.8 | 26.8 | 1392 |
| 1×95 | 3.0 | 1.5 | 21.0 | 23.5 | 0.3 | 1.7 | 25.7 | 28.8 | 1715 |
| 1×120 | 3.0 | 1.6 | 22.9 | 25.4 | 0.3 | 1.8 | 27.8 | 30.9 | 2097 |
| 1×150 | 3.0 | 1.7 | 24.5 | 27.2 | 0.45 | 1.9 | 30.3 | 34.0 | 2568 |
| 1×185 | 3.0 | 1.7 | 26.3 | 29.0 | 0.45 | 2.0 | 32.3 | 36.1 | 3050 |
| 1×240 | 3.0 | 1.8 | 29.0 | 32.2 | 0.45 | 2.1 | 35.2 | 39.1 | 3798 |

16	ADDISON	www.addison-cables.com

BS 6883&BS 7917 Caledonian Offshore & Marine Cables

MV Fire Resistant Power & Control Cables

www.caledonian-cables.co.uk

| Construction No. of cores×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Inner Sheath Thickness mm | Minimum Diameter Over Inner Sheath mm | Maximum Diameter Over Inner Sheath mm | Nominal Armour Wire Diameter mm | Nominal Outer Sheath Thickness mm | Minimum Overall Diameter mm | Maximum Overall Diameter mm | Approx. Weight kg/km |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1×300 | 3.0 | 1.9 | 31.6 | 34.8 | 0.45 | 2.2 | 37.9 | 41.9 | 4582 |
| 1×400 | 3.0 | 2.1 | 35.1 | 38.5 | 0.45 | 2.3 | 41.7 | 46.2 | 5533 |
| 1×500 | 3.2 | 2.2 | 38.7 | 42.6 | 0.45 | 2.5 | 45.7 | 50.4 | 6828 |
| 1×630 | 3.2 | 2.4 | 43.6 | 46.6 | 0.45 | 2.6 | 49.7 | 55.0 | 8712 |
| 3×25 | 3.0 | 1.9 | 30.9 | 34.1 | 0.45 | 2.1 | 37.1 | 41.1 | 2358 |
| 3×35 | 3.0 | 2.0 | 33.0 | 36.2 | 0.45 | 2.2 | 39.4 | 43.8 | 2747 |
| 3×50 | 3.0 | 2.1 | 35.8 | 39.1 | 0.45 | 2.3 | 42.3 | 46.9 | 3325 |
| 3×70 | 3.0 | 2.2 | 39.7 | 43.5 | 0.45 | 2.5 | 46.6 | 51.4 | 4274 |
| 3×95 | 3.0 | 2.4 | 43.7 | 47.7 | 0.45 | 2.7 | 51.1 | 56.4 | 5347 |
| 3×120 | 3.0 | 2.5 | 47.5 | 51.7 | 0.45 | 2.8 | 55.1 | 60.6 | 6493 |
| 3×150 | 3.0 | 2.7 | 51.1 | 55.7 | 0.45 | 3.0 | 59.0 | 65.1 | 7684 |
| 3×185 | 3.0 | 2.8 | 55.2 | 60.0 | 0.45 | 3.2 | 63.5 | 69.8 | 9213 |
| 3×240 | 3.0 | 3.1 | 61.2 | 66.6 | 0.45 | 3.4 | 69.9 | 76.8 | 11583 |
| 3×300 | 3.0 | 3.3 | 66.6 | 72.2 | 0.45 | 3.6 | 75.7 | 82.9 | 14031 |

www.addison-cables.com

ADDISON	17